TECHNICAL DATA SHEET. 		     TECHSPBLACK.DOC page 1 of 2

1.	IDENTIFICATION OF PRODUCT AND COMPANY

Product name : 	SP BLACK TOP

Hard black bituminous wax based self anti-corrosion

coating for ferrous and non-ferrous metals designed to meet

MIL-C-16173D-4 for automotive cavity protection and for use as

a heavy duty coating for steel sections in salt environments

and a topcoat for Navy Steel and other rust primers.

Note: SP Black Top is also available in a lower solids formulation as

SP Black Top 40

Company        :  	D. Adam & Associates  /  ACTEL Coatings

Clarendon, 17 High Cross Avenue, Melrose TD6 9SQ Scotland, U.K.

Tel: 07880 805478  www.actel.f9.co.uk   dougadam@globalnet.co.uk

2.	TECHNICAL DATA

2.1	STORAGE:		Store securely in original labelled containers at 0 to 25oC

away from oxidisers, naked flames and sources of ignition.

2.2	APPLICATION:		Apply by spray, brush or roller at  80. to give 40.  d.f.t

2.3	OVERCOATING:	A second coat can be applied after 8 hours but hi-build films

can be achieved with a single pass spray application.

SAF-T-SEAL can be used as a sealer before overcoating with a

solvent based colour coat to prevent “bleeding” through

2.4	DRYING TIME:		4 to 8 hours, very dependent on the drying conditions and w.f.t.

2.5	COVERAGE:		Theoretical  - up to 10 sq. metres per litre.

Practical      - 4 to 7 sq. metres per litre.

2.6	PACK SIZE:		5, 25 and 200 litres steel drums

2.7	DRY FILM:		40  from  80 wet film

2.8	FLASH POINT:		43oC.

2.9	SPECIFICATION:	Complies with MIL-C-83933A(MR) and MIL-C-62218 for rust 					preventative compounds for steelwork and MIL-C-16173D-4 for

motor vehicle cavity protection

2.10	STABILITY:		Normally stable. Avoid strong oxidisers and naked flames.

2.11	CORROSION TESTS:	Salt fog resistance ASTM-B 117		500 hours + at 40

Salt water immersion			Passes

Creep penetration after 7 days		Passes

  - OTHER PROPERTIES: Self healing film

Non sagging after spray applications

TECHSPBLACK.DOC page 2 of 2

3.	PREPARATION

  - SP BLACK TOP is supplied ready to use. Stir well before use. May be thinned to improve

spray properties and levelling in brush applications.

3.2	Ensure proper ventilation in confined areas.

3.3	Surfaces should be clean and free from surface dirt, dust, grease and any corrosion 	products.

3.4	Weathered steel should be high pressure water or wet abrasive blasted to SSOC-SP6.

  - Best results are achieved on rusted steel if it is first passivated by treating with Envirosteel

or primed with Navy Steel.

4.	APPLICATION

  - SP BLACK TOP should preferably be stored at room temperature (20oC/68oF) for 24 hours

before use.

Best applied by airless spray. SP BLACK TOP can also be applied by brush or roller.

4.2	Nominal coverage rates of 10m2 per litre are possible on smooth surfaces.

Actual coverage will be determined by the profile of the substrate to be coated and the dry

film thickness specified..

  - SP BLACK TOP will normally be touch dry within 4 to 8 hours depending on the temperature

and humidity. Cooler temperatures delay curing.

4.4	Wash brushes and equipment with white spirit immediately after use. Clean spray lines 	before SP BLACK TOP dries.

5.	HEALTH AND SAFETY

This product is flammable with a Flash Point of 43oC. Please ensure that operators 	read and understand the Health and Safety Data Sheet before using this material.

Revision dated 20th May ‘03