TECHNICAL DATA SHEET. 		TECHENVD.DOC Page 1 of 2

1.	IDENTIFICATION OF PRODUCT AND COMPANY

1.1	Product name : 	ENVIROGUARD CGR

Water based chewing gum release coating

1.2	Company        :  D. Adam & Associates / ACTEL Coatings

Clarendon, 17 High Cross Avenue, Melrose TD6 9SQ Scotland, U.K.

Tel: +44  (0) 7880 805478  E:  dougadam@globalnet.co.uk    www.actel.f9.co.uk

2.	TECHNICAL DATA

2.1	STORAGE:		Protect from freezing.

2.3	APPLICATION:             Apply a minimum of two full coats  by back pack compression
                                                   sprayer or until a mist spray of water "beads" on the dried treated 
                                                   surface. 
                                                   Application is very quick and simple.

2.4	OVERCOATING:	Enviroguard can be applied in mist coats, wet on wet in good drying 				conditions. Otherwise, recoat when touch dry.

2.5	DRYING TIME:	             2 to 8 hours, very dependent on the drying conditions.

2.6	COVERAGE:		Theoretical - to 15 sq. Metres per litre.

Practical     - 8 - 15 sq. Metres per litre.

2.7	PACK SIZE:		Cartons of 4 x 5 litres and 25 litre drums

2.8	FLASH POINT:	 None.

2.9	APPEARANCE:	When properly applied, Enviroguard is invisible on stone, brick
                                                   concrete and other building  materials.

2.10	REMOVAL:		Enviroguard can be removed by pressure washing using water at 				85oC or by using Cleanaway GTi followed by cold water.

2.11	THINNERS:		Clean water, only as required up to 20% for first coat or to improve

spray properties

3.	PREPARATION

3.1	Surfaces should be clean and free from surface dirt, gum, dust and grease.

3.2	All loose friable material should be removed and damaged areas made good.

3.3	Efflorescence and laitance should be treated as appropriate.

3.4	Existing mould growth should be treated and removed.

  - Where gum removal has been carried out, ensure that the area is well rinsed with water and

is touch dry

TECHENVD.DOC Page 2 of

4.	APPLICATION

4.1	Enviroguard as supplied is ready to use.

4.2	Apply Enviroguard when the air and surface temperature is between 5oC and 25oC and the 	relative humidity between 40% and 90%.

4.3	Use a fan spray tip on spray equipment to give an even spread of product. Only use brushes
             on smooth surfaces. Brushing on rough profiles can result in excessive aeration.

4.4	For spray work, application by backpack compression sprayer is recommended. It can also 	be applied by airless or air assisted sprayers in evenly applied fine mist coats using a 	maximum tip size of 0.017mm.

4.5	Apply at the recommended coverage rates.

4.6       On poured concrete or textured surfaces, take care to cover all of the surface irregularities 	and indents.

4.7	After use, all equipment should be cleaned by washing with warm soapy water. Dried product 	can be 	removed using hot water with a trace of household ammonia added.

5.	GUM REMOVAL

5.1	Chewing gum can easily be removed from treated surfaces as follows:

5.2	On heavily contaminated surfaces use a low pressure cold water washer to lift the gum.

5.3	Some areas may need minimal scraping with a blunt straight edge tool

  - Collect gum deposits for disposal in accordance with local regulations

5.5       Reapply one coat of Enviroguard after three or four few cleaning sessions or when it is 
            apparent that the coating is being walked off making gum removal slower than usual.

6.	HEALTH AND SAFETY

These products are considered to be non hazardous. However, please ensure that operators 	read and understand the health and safety data sheet before using these materials.

Enviroguard is a blend of waxes and acrylic polymers. It is water based, non flammable, non 
             toxic and non injurious to the environment

Revised May 2002